# Deck Cleaning and Care

# The deck surfaces require the correct maintenance and use to keep them in good shape for the future.

Below are a few line items and rules that are crucial for care, maintenance, and longevity:

All potted plants placed on the deck must have plastic feet/trivet/pedestal under them to encourage air flow and keep the deck surface from holding moisture.  Ideally a rolling pedestal will make cleaning and maintenance easy.  Pots should be moved periodically to allow for airflow where the feet rest.

If you are using retro/antique outdoor furniture, make sure the feet touching the deck surface has plastic feet on them.  If it gets hot enough this type of furniture can soften the deck coating and meld the furniture to the deck surface during the cooling process.

No carpets, rugs, tiles, or other floor/deck covering should be placed on the deck surface as they hold will moisture and deteriorate the deck surface at an accelerated rate.  Floor/Deck Coverings VOIDS OUR WARRANTY.  (Updated May 30, 2020)

Pets should not be allowed to defecate or urinate on the deck surface this will promote rapid decay of the membrane

Decks should be gently washed a couple times a year using either Simple Green.  Only soft scrub brushes should be used on the deck surface. (Updated May 30, 2020)

Below is from the Manufacturer’s Manual (Updated May 30, 2020)

CLEANING

Weekly - Sweep or rinse deck to remove loose debris and dirt.

Monthly - Thoroughly clean the deck to remove dirt, debris, oil or grease drippings, black tire marks, etc. Cleaning may be by:

(1) Scrubbing with a mild cleaner, such as Simple Green, or any other low suds, biodegradable detergent. Requires thorough rinsing to avoid being slippery when wet or stains from sun affecting detergent residue.

(2) High pressure water blast. (not greater than 1,000 psi at nozzle)

Avoid the use of strong solvents, especially hydrocarbon type solvents.

- If you notice any cracks or breaches in your deck surface notify the Board/Management right away.

- Nothing should be screwed into the deck surface or into or attached to the walls of your deck or the building.

- Care should be taken so that you do not drop any heavy objects or sharp objects on the decks surface.  If any accidents happen, they should be reported to The Board/Management immediately so that the proper repair can be completed

Thank you for your cooperation.

The Courtyard Board

May 30, 2020